High-temperature, high-pressure hydrothermal synthesis, crystal structure, and infrared and NMR spectroscopy of a barium lead borate

AAA (壁報或口頭報告者), BBB(共同作者) and DDD (指導教授)*

Department of Chemistry, National Central University, Jhong-Li, Taoyuan,

Taiwan 32001

abcdef@cc.ncu.edu.tw

With a high-temperature, high-pressure hydrothermal technique, a new barium lead borate, [Ba3Pb(H2O)][B11O19(OH)3] (1), has been synthesized and characterized by single-crystal X-ray diffraction, and infrared and solid-state NMR spectroscopy.1 The structure of 1 contains planar thick layers of borates with the Ba2+ cations at sites in the inter- and intralayer space.2

Structure of 1

References

[1]. (a) Jen, I.-H.; Lee, Y.-C.; Tsai, C.-E.; Lii, K.-H.*. Inorg. Chem. 2019, 58, 4085.

(b)

[2]. Keszler, D. A. Borates: Solid State Chemistry. In Encyclopedia of Inorganic Chemistry; King, R. B., Ed.; John Wiley & Sons: Chichester, 1994, Vol. 1, pp 18−327.

|  | 報告者簡歷 國立中央大學碩士班二年級 其他有助於認識你與你的化學相關資訊 |
| --- | --- |

相片